Check List BEFORE Using Abrasive Cut-Off Saw

- Research hardness of material before cutting. Change the blade according to the hardness of the material. Hard materials include: metal carbides; metal borides; hardened tool steels; and ceramics. Soft materials include: carbon alloy steels; alloy steels; cast irons; and non-ferrous alloys. Boxes have labels as to which blade cuts what type of material.

- Visually inspect all wheels before mounting for possible damage. Do NOT use a cracked or chipped wheel or one that has been dropped or has become damaged in any way. If deemed unusable give them to Christine in the machine shop.

- Do NOT force a wheel onto the machine or alter the size of the mounting hole. If the wheel does not fit, get one that does.

- Do NOT tighten the mounting nut excessively.

- Allow the newly-mounted wheel to spin at operating speed for a minute with the shield down before cutting or grinding.

- Before operating, check the machine speed against the established maximum safe operating speed marked on the wheel. Do NOT ever exceed the maximum operating speed established for the wheel.

- While cutting, turn off the coolant before stopping wheel to avoid creating an out-of balance condition which could cause the blade to fail.

- Always have the safe guard down before turning on the cut-off wheel and leave down until wheel has stopped moving.

- Store cutting wheels horizontally.